Supporting information

Sepiolite nanofibers decorated with Zn single sites: a sustainable filler for mechanically robust and self-healing ionomeric elastomer composites.

Paolo Valagussaa, Silvia Mostoni*a, Marianella Hernandez Santanab, Itziar Mas Ginerb, Michele Mauria, Roberto Simonuttia, Sandra Diréc, Emanuela Callonec, Barbara Di Credicoa, Roberto Scottia, Massimiliano D’Arienzoa

a Department of Materials Science, INSTM, University of Milano-Bicocca, Via Roberto Cozzi 55, Milano, Italy

b Institute of Polymer Science and Technology (ICTP), CSIC, C/ Juan de la Cierva, 3, Madrid, Spain

c “Klaus Müller” Magnetic Resonance Lab., Department of Industrial Engineering, University of Trento, Via Sommarive 9, 38123 Trento, Italy

TGA calculations

First, the moles of –OH per gram of base-treated Sep (nOH) were calculated from the weight loss in the 150–1000 °C temperature range (∆W150-1000°C) of Sep-OH, considering that each molecule of water released corresponds to the condensation of two hydroxyl groups:

ΔW150-1000°C = 12 · (nOH · wSep-OH(1000°C)) · MWH2O  		     Eq. S1

nOH = 2ΔW150-1000°CMWH2O∙wSep-OH(1000°C)			     Eq. S2

where wSep-OH(1000°C) is the sample mass at 1000 °C and MWH2O is the molecular weight of water (18.01 g/mol). Weight loss below 150 °C is assumed to arise from desorption of physisorbed species, such as solvent molecules. Based on this calculation, nOH = 8.85 mmol/g.

The increased weight loss observed for Sep@APTES in the 150–1000 °C range is attributable to the higher organic content relative to Sep-OH. This increase is hypothesized to originate from: (i) combustion of –CH₂CH₂CH₂NH₂ functional groups from APTES; (ii) desorption of water from the remaining silanol groups, considering that two –OH groups are replaced for each silane molecule attached to the sepiolite surface; and (iii) desorption of water from –OH groups of APTES formed by hydrolysis of the residual ethoxy group.

Accordingly, the weight loss can be expressed as:

ΔW150-1000°C = nR · MWR+ (nOH · wSep-APTES(1000°C) - 2nR)·MWH2O2+(nOH-A · MWH2O)2    	 Eq. S3

where MWR is the molecular weight of –CH2CH2CH2NH2, nOH-A is the number of hydroxyl groups bound to each APTES unit (equal to nR), and the factor 1/2 accounts for the condensation of two –OH groups into one water molecule.

From the moles of –CH2CH2CH2NH2, (nR), the weight percentage of aminopropyl groups (WAP%)  is calculated as:

wAP% =  nR · MWR mSep-APTES(1000°C)· 100		                Eq. S4

DSC with stearic acid

DSC tests were carried out using a three-steps temperature program:

- from 25 to 200 °C, heating rate of 5 °C/min, adding an isotherm of 2 min at 200 °C;

- temperature was brought back to 25 °C (heating rate -10 °C/min), adding an isotherm of 2 min at 30 °C;

- second heating step from 25 to 200 °C (heating rate 5 °C/min), followed by an isotherm of 2 min at 200 °C;

- final cooling treatment to 25 °C (heating rate -10 °C/min).

All the experiments were carried out under nitrogen flow of 80 mL/min.

Preparation of Sep@ZnO filler

Sep-OH filler was decorated with ZnO nanoparticles by preparing a 0.10 M NaOH solution in 70 mL of EtOH at 65°C. After complete NaOH dissolution, 0.33 g of zinc acetate dihydrate (Zn(CH3COO)2·2H2O) was added and stirred for 20 min. Subsequently, 1.0 g of Sep-OH was added, and the suspension was left under stirring for additional 20 min at 65 °C. After cooling, the product was isolated trough centrifugation (9000 rpm, 20 min) and washed twice with EtOH. The resulting solid was dried at 80 °C overnight.

XRD

Figure S1. XRD patterns of Sep@APTES-Zn compared to bare Sep-OH.

N2 physisorption

Figure S2. Nitrogen physisorption isotherms at 77K for a) Sep-OH, b) Sep@APTES and c) Sep@APTES-Zn.

FTIR

Figure S3.  ATR/FTIR spectra of APTES and Zn(NO3)2 precursors.

Solid State NMR

Figure S4.  29Si CPMAS NMR spectra of Sep-OH and functionalized Sep samples.

SEM

Figure S5.  SEM micrographs of Sep@APTES-Zn at different magnifications.

Electron Paramagnetic Resonance (EPR) spectroscopy

Figure S6. EPR spectrum of Sep@APTES-Zn/Cu prepared by substituting Zn(II) with Cu(II) (0.01%); the inset shows the Peisach–Blumberg correlation diagram for oxygen and nitrogen coordinating Cu(II) ions.

TGA of XNBR NCs

Figure S7. TGA curves of a) XNBR/Sep-X and b) XNBR/Sep@APTES-Zn-X NCs. In both graphs the grey curve is the reference XNBR NC prepared by using ZnO as reported in Table 1 of the main text.

Mechanical properties

Table S1. Parameters of the curing curves registered for XNBR/Sep-X, XNBR/Sep@APTES-ZnX and XNBR NCs. In the first three colums the kinetic parameters are reported: tS1, tS2 and tS90 represent the time required to achieve 1 %, 2% or 90 % of the maximum torque. In the latter three columns the torque increase (ΔM), calculated as the difference between the maximum (MH) and the minimum torque (ML) are also shown.

Table S2. Parameter of the tensile tests performed on XNBR/Sep-X, XNBR/Sep@APTES-Zn-X compared to XNBR and XNBR/Sep@ZnO-10. In the Table the values of the measured stress at 100 % (M100), 300 % (M300) and 500 % (M500) strain, along with the values of tensile strength (TS) and elongation at break (EB) are reported.

Self-Healing properties

Table S3. Healing efficiency (η, %) calculated from TS values of the healed and pristine NCs, according to Eq. 1 of the main text.

Table S4. Healing efficiency (η, %) calculated from EB values of the healed and pristine NCs, according to Eq. 1 of the main text.

Time Domain NMR

Three-component decay function used for fitting Hahn Echo experiments at 30 °C:

y=A exp- x2D+B exp- xT2b+C exp- xT2c			Eq. S5

Where A, B and C represent three distinct proton populations, corresponding to microstructural domains within the composite. These can be described as a highly constrained fraction (A), a slightly constrained fraction (B) and a mobile fraction (C). The parameter D represents the gaussian relaxation constant of the rigid cross-linked domains and ionic clusters. The parameter T2b and T2c denote the relaxation time constants associated with the semi-mobile entangled segments and the highly mobile free chains within the XNBR matrix, respectively.

Table S5. Exponential function parameters of XNBR/Sep@APTES_N, XNBR/Sep@APTES-Zn-10_N and XNBR/Sep@ZnO-10_N NCs, according to Eq.S5.